## Slide 1: Effects of interdiffusion on Cu/Ni semi-coherent interface properties
Alex Selimov1, Kevin Chu1, David L. McDowell1
1School of Materials Science and Engineering Georgia Institute of Technology
October 11, 2022

## Slide 2: Overview
Motivation
Methodology
Results
  Effects of interdiffusion on misfit dislocation structures
  Solute cluster and solute segregation
  Effects of solute concentration on interface shear strength
  Microrotation vector analysis of interface deformation
  Qualitative comparison of energy barriers for interface sliding
Conclusions

## Slide 3: Nanolaminates offer improved properties relative to bulk constituents
Wang, J., Zhou, Q., Shao, S., & Misra, A. (2017). Materials Research Letters, 5(1), 1-19.
Nasim, M., Li, Y., Wen, M., & Wen, C. (2020). Journal of Materials Science & Technology, 50, 215-244.

## Slide 4: When constituents are miscible, interfaces are diffuse due to interdiffusion of chemical species
Layer composition can be controlled through annealing1
Accumulative roll bonded multilayer shows alloyed layers2
1Yan, X. L., Liu, Y., Swart, H. C., Wang, J. Y., & Terblans, J. J. (2016). Applied Surface Science, 364, 567-572.
2Sun, Y., Chen, Y., Tsuji, N., & Guan, S. (2020) Journal of Alloys and Compounds, 819, 152956.

## Slide 5: Diffuse interface structures can lead to improved mechanical properties
Wang, C. J., Yao, B. N., Liu, Z. R., Kong, X. F., Legut, D., Zhang, R. F., & Deng, Y. (2020). International Journal of Plasticity, 131, 102725.
Chen, Y., Li, N., Hoagland, R. G., Liu, X. Y., Baldwin, J. K., Beyerlein, I. J., ... & Mara, N. A. (2020).. Acta Materialia, 199, 593-601.

## Slide 6: Explicit consideration of misfit dislocation density changes is required.
Moszner, F., Cancellieri, C., Chiodi, M., Yoon, S., Ariosa, D., Janczak-Rusch, J., & Jeurgens, L. P. H. (2016). Acta Materialia, 107, 345-353.
Chladek, M., Dorner, C., Buchal, A., Valvoda, V., & Hoffmann, H. (1996). Journal of applied physics, 80(3), 1437-1445.
Wang, C. J., Yao, B. N., Liu, Z. R., Kong, X. F., Legut, D., Zhang, R. F., & Deng, Y. (2020). International Journal of Plasticity, 131, 102725.
Small change in lattice parameters should lead to significant changes in interface misfit structure

## Slide 7: Overview
Motivation
Methodology
Results
  Effects of interdiffusion on misfit dislocation structures
  Solute cluster and solute segregation
  Effects of solute concentration on interface shear strength
  Microrotation vector analysis of interface deformation
  Qualitative comparison of energy barriers for interface sliding
Conclusions

## Slide 8: Cu/Ni bicrystals are created with both lower misfit density and presence of solutes
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 9: Methodology for developing model geometries
1. Generate individual Cu/Ni layers with concentration dependent lattice constant.
2. Randomly swap atoms in each layer until desired solute concentration.
3. Stack each layer.
4. Run hybrid MC/MD at 700 K until reasonable convergence.

## Slide 10: Hybrid Monte-Carlo/Molecular Dynamics used to generate diffuse interface structures
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 11: Microrotation vector is defined from the atomic deformation gradient
Microrotation defined by1:
where
from
1Tucker, G. J., Zimmerman, J. A., & McDowell, D. L. (2011). International journal of engineering science, 49(12), 1424-1434.

## Slide 12: Microrotation analysis used to analyze interface deformation
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.
Magnitude of vector relates to deformation:
0.07 – Dislocation Glide
0.18 – Grain Boundary Migration

## Slide 13: Overview
Motivation
Methodology
Results
  Effects of interdiffusion on misfit dislocation structures
  Solute cluster and solute segregation
  Effects of solute concentration on interface shear strength
  Microrotation vector analysis of interface deformation
  Qualitative comparison of energy barriers for interface sliding
Conclusions

## Slide 14: Primary difference in interface structure is the misfit dislocation density
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 15: Stacking fault energy of the interface may not significantly change for diffuse interfaces
No clear trend in energy
Decrease may result from dislocation curvature
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 16: Solutes are not observed to form clusters at the interface
Decrease
Decrease
Increase
*Calculated using Ovito1
1Stukowski, A. (2009). Modelling and simulation in materials science and engineering, 18(1), 015012.
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 17: Solutes preferably segregate to misfit nodes and to misfit dislocations
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 18: Stress-strain response exhibits improved shear strength with interdiffusion
Distributed maximum shear stresses
20% is outlier
Median values are similar
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 19: Larger maximum node displacements are observed with interdiffusion. Larger spread in values implies distributed energy barriers.
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 20: Microrotation maps reveal non-uniform interface deformation
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.
Higher local deformation

## Slide 21: Microrotation magnitudes correspond to node displacements
Linear trend between node displacement and average microrotation
20% exhibits larger microrotation sum for node displacement
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 22: Node displacement and node microrotation does not depend on the local solute fraction
Longer range configuration between interface solutes and interface misfits may be more important
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 23: Interface deformation is primarily constrained to misfit nodes. Increase in range may be due to distributed resistance
20% exhibits highest median misfit dislocation and misfit node deformation
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.
Maximum microrotations go up

## Slide 24: Energy change per node supports distributed energy barriers for diffuse interfaces
aaa
20% remains outlier
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 25: Difference in energy may be due to the activation of misfit dislocation glide
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 26: Comparison of energy changes for only misfit node glide leads to expected trend.
Higher barrier indicates misfit node glide is the rate-limiting process in interface sliding
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 27: Conclusions
Interdiffusion leads to slight increases in shear strength of Cu/Ni nanolaminates.
Local solute concentration does not correlate with localized interface deformation indicating the importance of longer-range structure. Need description of longer-range structure.
A switch from uniform interface sliding to localized interface sliding is observed based on distributed energy barriers.
Misfit node glide facilitates misfit dislocation glide and is the rate-limiting step in the process.

## Slide 28: Acknowledgements
This work is based on research supported by the National Science Foundation under the Grants CMMI-1761553.
All presented simulations were conducted using XSEDE resources under the allocation TG-MSS150010.

## Slide 29
Thank you! Questions?

## Slide 30: Interface excess volume analysis1 used to track evolution of misfit dislocation structure
Locally high excess volume attributed to misfit node
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.
1Shao, S., Wang, J., & Misra, A. (2014). Journal of Applied Physics, 116(2), 023508.