## Slide 1: Concurrent Atomistic-Continuum studies of confined layer slip in Cu/Ni nanolaminates
Alex Selimov1, Youping Chen2, David L. McDowell1
1School of Materials Science and Engineering Georgia Institute of Technology
2Dept. Mechanical and Aerospace Engineering University of Florida
October 6, 2022

## Slide 2: Overview
Motivation
Methodology
Results
  Dislocation Generation Mechanisms
  Dislocation/Interface Interactions
  Energetics of Confined Layer Slip
Conclusions

## Slide 3: Nanolaminates offer improved properties relative to bulk constituents
Wang, J., Zhou, Q., Shao, S., & Misra, A. (2017). Materials Research Letters, 5(1), 1-19.
Nasim, M., Li, Y., Wen, M., & Wen, C. (2020). Journal of Materials Science & Technology, 50, 215-244.

## Slide 4: Confined Layer Slip (CLS) is a fundamental deformation mechanism for nanolaminate materials
Misra, A., Hirth, J. P., & Hoagland, R. G. (2005). Acta materialia, 53(18), 4817-4824.
Li, N., Wang, J., Misra, A., & Huang, J. Y. (2012), 18(5), 1155-1162.
Has been observed experimentally

## Slide 5: Consideration of interface evolution is important for accurate models of CLS
*Treats interfaces as perfect sinks
Chen, T., Yuan, R., Beyerlein, I. J., & Zhou, C., International Journal of Plasticity 124 (2020) 247-260.

## Slide 6: But modeling small interface segments with periodic boundary conditions constrains interface evolution multiscale modeling
Shao, S., Wang, J., Beyerlein, I. J., & Misra, A. (2015). Acta Materialia, 98, 206-220.
Selimov, A., Xu, S., Chen, Y., & McDowell, D. (2021). Journal of Materials Research, 36(13), 2763-2778.

## Slide 7: Overview
Motivation
Methodology
Results
  Dislocation Generation Mechanisms
  Dislocation/Interface Interactions
  Energetics of Confined Layer Slip
Conclusions

## Slide 8: The Concurrent Atomistic-Continuum (CAC) method
Key points:
Coarse-graining reduces degrees of freedom.
Atomistic resolution preserves solution accuracy in certain regions as desired.
Integral form finite element formulation accommodates dislocations in mesh discontinuities.
2NN elements fully capture dislocation stacking faults.
S. Xu et al., International Journal of Plasticity 72 (2015).

## Slide 9: CAC finite element mesh and model geometry
CAC Mesh
CG domain
CG domain
CG domain
AT domain
AT domain
Cu
Ni
Ni
Model Dimensions:104 x 90 x 47 nm
Degrees-of-Freedom: 12,944,073
Atoms in equivalent atomistic model: 38,476,569
Periodic in all dimensions
Onat Cu/Ni Potential1
1Onat, B., & Durukanoğlu, S., Journal of Physics: Condensed Matter 26(3) (2013) 035404.

## Slide 10: Relaxed semi-coherent interface structure for models under investigation
Selimov, A., Chu, K., & McDowell, D. L. (2022). International Journal of Plasticity, 157, 103393.

## Slide 11: Loading conditions selected to isolate single dislocation loop
See also: Zhang, R. F., Wang, J., Beyerlein, I. J., & Germann, T. C., Scripta Materialia 65(11) (2011) 1022-1025.
*Loading parallel to interface plane
Unload…
Apply Shear …

## Slide 12: Stress-strain response for geometry
Lattice dislocation impinges on top interface
Hysteresis due to “freezing” interface segment

## Slide 13: Overview
Motivation
Methodology
Results
  Dislocation Generation Mechanisms
  Dislocation/Interface Interactions
  Energetics of Confined Layer Slip
Conclusions

## Slide 14: Dislocation generation mechanism exhibits non-Schmid effects
Slip System | Schmid Factor
 | 0.314
 | 0.393
 | 0.079
 | 0.314
 | 0.079
 | 0.393
 | 0.314
 | 0.157
 | 0.157
Slip System | Schmid Factor
 | 0.314
 | 0.393
 | 0.079
 | 0.314
 | 0.079
 | 0.393
 | 0.314
 | 0.157
 | 0.157
See also: Chen, X. Y., Kong, X. F., Misra, A., Legut, D., Yao, B. N., Germann, T. C., & Zhang, R. F., Acta Materialia, 143 (2018) 107-120.

## Slide 15: Dislocation generation on intersecting slip planes accompanies development of threading dislocation
Multiple threading dislocations form on same plane

## Slide 16: Misfit dislocations are primary obstacles to slip transmission

## Slide 17: Multiple threading dislocations form on initial glide plane

## Slide 18: Interaction between CLS dislocation and misfit nodes leads to change of interface structure
Cu side of interface

## Slide 19: Confined layer slip leads to development of interface disconnection
Ni side of interface
Constriction of misfit dislocation pattern corresponds to stair-rod dislocation
Step deposited at interface by threading dislocation

## Slide 20: Approximate comparisons of energy barriers by tracking ΔE for participating atoms
Aγ
Cδ
Initial
Final

## Slide 21: Threading dislocation facilitates generation of γA dislocations

## Slide 22: Interface energetics reveal the fundamental role of misfit dislocations in resisting slip transmission
Step atoms
Leading Partial Interaction
Trailing Partial Interaction
Misfit node
atoms

## Slide 23: Conclusions
Multiple threading dislocations can form on the same initial slip plane; interface evolution will impact subsequent glide.
Threading dislocation interactions leads to expanded misfit node structure which facilitates emission of dislocations on intersecting slip planes.
Ideal Cu/Ni interface structure cannot accommodate CLS due to low slip transmission.
Creation of interface step has lower energy cost than the misfit node structure changes.

## Slide 24: Acknowledgements
This work is based on research supported by the National Science Foundation under the Grants CMMI-1761553.
All presented simulations were conducted using NSF XSEDE resources under the allocation TG-MSS150010.

## Slide 25
Thank you! Questions?

## Slide 26: Coarse-graining affects dislocation core structure, long range fields preserved
Stress fields match well with different FE sizes1
Linear interpolation in FEs smears dislocation core1
1S. Xu et al., International Journal of Plasticity, vol. 72, 2015.

## Slide 27: Cu/Ni exhibits characteristic spiral interface pattern

## Slide 28: Microrotation analysis of semi-coherent Cu/Ni interfaces